MoGe Target Info.

Last updated

04/01/2009

SuperConductorMaterials, Inc.

(800) 932-9333 / 845-368-0240

www.scm-inc.com

Material: Mo/Ge(76:24 at %) target

Description: 2” dia x 0.125” thick  complete with Copper(Cu) backing plate plus Indium(In)  bonding

Purity of M0 :99.99%

Purity of  Ge: 99.999%